Electrocatalytic Properties of Sb2Se3 Thin Films for Water Electrolysis

Vusala Majidzade1, Sevinj Javadova1, Samira Jafarova1, Sh.O. Eminov2, Akif Aliyev1

and Dilgam Tagiyev1

1Institute of Catalysis and Inorganic Chemistry, Baku, Azerbaijan

2Institute of Physics, Baku, Azerbaijan

Water electrolysis is the most attractive method for obtaining environmentally friendly hydrogen. As you know, during the electrolysis of water, water molecules are separated into hydrogen and oxygen molecules using a current flowing through water. This process requires quite a lot of energy, so the use of electrocatalysts can significantly increase the efficiency of this process.

Research is often carried out in the field of electrocatalysis of metal chalcogenides as a cathode in the electrolysis of water [1]. In particular, antimony selenide (Sb2Se3) [2] is a semiconductor material that has been studied as a potential electrocatalyst for hydrogen evolution during water electrolysis. The electrocatalytic properties of Sb2Se3 thin films during water electrolysis have been studied in several studies. These studies have shown that Sb2Se3 exhibits good catalytic activity in the hydrogen evolution reaction (HER). The researchers attributed this activity to the high conductivity and good stability of the Sb2Se3 film.

Fig.1 . X-ray phase analysis of Sb2Se3 thin films

In general, the electrocatalytic properties of Sb2Se3 thin films in the electrolysis of water open up prospects for the development of efficient and stable cathodes in the process of water and hydrogen ion reduction. However, more research is needed to optimize the synthesis and performance of this material.

For the study of the electrocatalytic characteristics, thin Sb2Se3 semiconductor films were obtained by electrochemical deposition from an aqueous and organic electrolyte with a tartrate additive. The samples were obtained on a nickel substrate with an area of 2 cm2. XRD pattern of  Sb2Se3 is shown in Fig.1

Catalytic studies of Sb2Se3 thin films were carried out in a neutral medium (0.5 M Na2SO4). The polarization curves were recorded in an IVIUMSTAT Electrochemical Interface potentiostat (Ivium Technologies). A glass three-electrode electrochemical cell with a volume of 100 ml was used. To compare the catalytic activity of different substrates, Ni with an area of 2 cm2, Pt with an area of 0.35 cm2, and samples of heat-treated Sb2Se3 films with an area of 2 cm2 were used. The auxiliary electrode used is a platinum plate with an area of 4 cm2. The reference electrode was a silver chloride electrode – (Model No. CS901, CorrTest Instruments).

Fig.2 Electrocatalytic activity of synthesized Sb2Se3 thin films in a neutral medium (0.5 M Na2SO4).

As can be seen from Fig.2 compared with other cathodes, annealed Sb2Se3 has high electrocatalytic activity. Annealing of samples on a nickel electrode was carried out at a temperature of 723 K, in an atmosphere of inert gas - argon 70 minutes. The increase in electrocatalytic activity is due to changes in the structure of the studied material during heat treatment. This can lead to an increase in the number of active sites, or reduce the impurities' content and improve the material's crystal structure.

Acknowledgment

The study was ﬁnancially supported by the National Academy of Sciences of Azerbaijan within the framework of research programs in priority directions in 2019–2022.

References

- Marsagishvili, T.A. et al. Chemical Problems, 19, 7-17 (2021)

- Majidzade,V.et al. Chemical Problems, 18, 181-19 (2021)